IrCoPt

- Multilayerstack: Pt(10.2nm)Co(0.6nm)Pt(1.2nm) [Ir(1.2nm)Co(0.6nm)Pt(1.2nm)]x10 Pt(3nm)

- 11 magnetic Co layers with the thickness 0.6nm add up to a total of 6.6nm

- The sample has a total thickness of 45 nm and is 200nm wide in the x- and y-direction

- Saturation magnetization: 0.956e6 A/m

- Exchange constant: 10e-12 J/m

- Uniaxial anisotropy constant in J/m^3: 0.65e6, 0.7e6, 0.75e6, 0.8e6

- DMI constant in J/m^2: 1.5e-3, 1.7e-3, 1.9e-3, 2.1e-3

- Diameter of the skyrmion with varying anisotropy: 62.5nm (0.65e6), 49.4nm (0.7e6), 33.4nm (0.75e6), 18.7nm (0.8e6)

- Diameter of the skyrmion with varying DMI: 33.8nm (1.5e-3), 49.4nm (1.7e-3), 61.3nm (1.9e-3), 71.6nm (2.1e-3)

- 80 mT applied external field in -z-direction

- The stray field in Tesla of the skyrmion is taken 100nm above the sample surface and 100nm below the sample surface. Watch out the sample is not symmetric!