FeGd

- Multilayer stack: FeGd(60nm)

- The sample has a total thickness of 60 nm and consists only of magnetic FeGd multilayers

- The sample is 201 cells wide in the x- and y-direction. The center of the sample and the center of the skyrmion is at 1e-7 in x-direction and 1e-7 in z-direction.

- Saturation magnetization: 225e3 A/m

- Exchange constant: 6e-12 J/m

- Uniaxial anisotropy constant in J/m^3: 22.4e3

- DMI constant in J/m^2: no DMI

- Diameter of the skyrmion with varying Ms (100-112%):

- 40nm (100%)

- 50nm (102%)

- 58nm (104%)

- 64nm (106%)

- 70nm (108%)

- 74nm (110%)

- 78nm (112%)

- 90 mT applied external field in +z-direction

- The stray field in Tesla of the skyrmion is taken 100nm above the sample surface and 100nm below the sample surface. The sample is symmetric!